## Slide 1
Tingwen Lia,c , William Rogersa , Douglas McCartyb, Jenny Tennanta
a: National Energy Technology Laboratory, Morgantown, WV
b: Southern Company Services, Wilsonville, AL
c: URS Corporation, Morgantown, WV
Computational Fluid Dynamic Simulations of a Pilot-Scale Transport Gasifier Using Mississippi Lignite Feedstock
2014 Gasification Technologies Conference

## Slide 2: Outline
Objectives
Introduction to Power Systems Development Facility ( PSDF ) & Transport Integrated Gasification ( TRIGTM )
The Modeling Tools
Model Setup
Simulation Results
Conclusions
2

## Slide 3: Objectives
Use data available from PSDF TRIGTM operations to validate NETL Computational Fluid Dynamic (CFD) models and chemical kinetics tools
Demonstrate the capability of NETL CFD tools to model gasifier performance over a wide range of operating conditions
  Demonstration with Mississippi lignite fuel
  Build on previous simulations for bituminous and low rank coals
Provide insight to guide the continued development and validation of computational tools to support gasifier designers and operators
3

## Slide 4: Power Systems Development Facility
Power Systems Development Facility (PSDF)
  Test center sponsored by the U.S. Department of Energy (DOE) dedicated to the advancement of clean coal technology
    major areas of testing involve pressurized solids handling systems, coal gasifier optimization using a variety of fuels, and syngas conditioning
    home of the National Carbon Capture Center
    features key components of an IGCC plant
4
www.nationalcarboncapturecenter.com

## Slide 5: Transport Integrated Gasifier (TRIGTM)
TRIGTM (Transport Integrated Gasification)
  Developed by KBR, Southern, and DOE
    Based on KBR FCC technology
  Air- and oxygen-blown
  Good for low-rank coal
  Major components:
    Mixing zone
    Riser
    Cyclone/disengage, loop-seal
    Standpipe, J-leg
5
TRIGTM Schematic
www.kbr.com

## Slide 6: The Modeling Tools
  The NETL MFIX (Multiphase Flow with Interphase eXchanges) Computational Fluid Dynamics Code is the basis
  MFIX is NETL’s open-source CFD software platform for hydrodynamics, heat transfer, and chemical reactions in multiphase systems
  MFIX provides transient, 3D predictions of pressure, velocity, temperature, and species for all phases
The NETL C3M (Carbonaceous Chemistry for Computational Modeling) is used for determining the coal reaction mechanism
  C3M is chemistry management software focused on computational modeling of reacting systems
  Provides direct links between kinetic information and CFD
  Virtual kinetic laboratory – allows evaluation of complex kinetic expressions
Simulations are performed on the NETL Supercomputer
  Ranked in top 100 supercomputers in the world
6
Notes: This slide summarizes the basic model components. The simulation was conducted by using NETL’s open-source code MFIX which has been widely used for gas-solid flow modeling.
3800 registered users, 73 countries
68% university
18% industry
4% other labs
10% other

## Slide 7: The MFIX Model Setup
Simulation with Detailed Setup
  Fine grid: 1.3 Million Computational Cells
  Well-resolved inlets & outlet for all streams
  Two solid “phases” used for coal and recycled ash with different sizes & densities
  Although high geometric fidelity, model is expensive to run
    long simulation time
    large datasets to manipulate
Created Simplified Setup
  Compared this to Detailed Setup results to verify acceptable accuracy
  Now able to do more simulations over a range of operating conditions
7
Simulation Geometry – To Scale
Detail of Inlets

## Slide 8: The MFIX Model Setup
Simplified Setup
  Coarse grid: 400,000 computational cells
    Major inlets & outlets are still well resolved
    Point sources near walls used to capture smaller inlet flows
  Single representative solid phase for coal and recycled ash
  A ‘filtered’ model used for momentum, heat & mass transfer to capture subgrid-scale physics
  Resultant model is much less expensive to run – still retains the major flow features
  Comparison to Detailed Case is very good
    Temperature and outlet composition are close
Li et al. Energy & Fuels, 2013, 27, 7896-7904.
8
Notes: SMD = Typical values are around 80 microns
Filtered model – based on Igci model
Filtered approach analogous to various turbulence models where you don’t resolve the scale of the turbulence, but you model the effects turbulence has on the flow

## Slide 9: Chemical Kinetics
Detailed coal devolatilization and gasification reaction kinetics were developed for Mississippi lignite
  17 gas-phase species and 4 solids-phase components are tracked
  Use the PC Coal Lab database through C3M to determine rate constants
    This approach accounts for the effects of local bed conditions and feed stock properties on the kinetics
  Thermodynamic properties provided by C3M from standard databases
Other reactions included in the scheme
  Char combustion: shrinking core model
  Gas phase combustion: global reaction mechanisms for hydrocarbons
  Water-gas shift: combination of catalytic and non-catalytic kinetics
Chemical kinetics parameters were held constant for all simulations
  No ‘tweaking’ of parameters was done to improve agreement
Van Essendelft et al. Advanced Chemistry Surrogate Model Development within C3M for CFD Modeling, Part 1: Methodology Development for Coal Pyrolysis, I&ECR 2014, 53, 7780-7796
Westbrook and Dryer, Simplified Reaction Mechanisms for the Oxidation of Hydrocarbon Fuels in Flames, Combustion Science and Technology, 1981, Vol. 27, pp. 31-43.
Notes: Westbrook and Dryer (1981) mechanisms for HC fuels
gas phase species: considered
O2, CO, CO2, CH4, H2, H2O, N2, Tar, Soot, PAH, OIL, H2S, C3H6, HCN, C2H4, C2H6, SO3
solid species:
char, volatiles, moisture, ash
PCCL is run over many conditions of temperature, pressure, gas composition, particle diameter to produce a gasification rates at each of these conditions
The thermo properties for most species are from the Burcat's database.
Tar, volatiles, ash, PAH and OIL, we have to calculate them based on their composition. Use the method developed by Dirk to calculate the heat of formation, heat capacity etc.
Initially, the experimental data we found on lignite was used to calibrate the PCCL runs. However, the results were far off. After that, I turned off the calibration and use the default factor recommended by PCCL.
No tweaking of rate constants:
NO. What I did is very similar to Mehrdad. Basically, I ran many PCCL runs covering a wide range of operating conditions (different gas compositions for gasification), then fitted the rate from those runs. The same rate expression was used for all PSDF runs.
Shrinking core model – from MGAS
Water-gas shift – switch between catalytic and non-catalytic rates based on solids content

## Slide 10: PSDF Tests using Mississippi Lignite
Operating conditions that were simulated – 11 Runs
  Gasifier temperature (~1600-1750F)
  Pressure (~191-211 psig)
  Steam-to-coal ratio (~0.005-0.174)
  Coal feed rate (~3500-4340 lb/hr)
  Lignite coal composition used for the simulations (after drying):
10
Proximate analysis |  | Ultimate analysis | 
Fixed carbon (%) | 31 | Carbon (%) | 46
Volatile matter (%) | 37.1 | Hydrogen (%) | 3.5
Moisture (%) | 17.1 | Oxygen (%) | 17.1
Ash (%) | 14.8 | Nitrogen (%) | 1
 |  | Sulphur (%) | 0.6
POWER SYSTEMS DEVELOPMENT FACILITY TOPICAL REPORT: GASIFICATION TEST CAMPAIGN TC25, 2008
Notes: Range of the 11 runs that were simulated

## Slide 11: Visualization of Transient Results
11

## Slide 12: Comparison of Model and Operating Data
Time-averaged model predictions were used for comparison with data
  e.g. Time history of syngas composition at riser exit for one case
12
Time average window

## Slide 13: Comparison of Model and Operating Data
Time-averaged pressure drop values – parity plots comparing prediction to measurement
Above the Lower Mixing Zone (LMZ), measured and predicted pressure data are in good agreement, with maximum discrepancy < 30%
Pressure drop values for the LMZ are excluded here - the simulation consistently underpredicts pressure drop in LMZ
13
LMZ
Notes: How much lower were dP / holdup in the LMZ?

## Slide 14: Comparison of Model and Operating Data
Time-averaged Temperature at varying height
Temperature profiles are in good agreement with measurements
Lower Mixing Zone temperatures from the model are slightly higher than data
  Model overpredicts carbon and resultant combustion in LMZ

## Slide 15: Comparison of Model and Operating Data
Time-averaged syngas composition at riser exit
15
Predicted exit syngas compositions are in good agreement with measurements - with most discrepancies within 20%.
Predicted
Measured
Run #1
Run #2
Run #3
Run #4
Run #5
Run #6
Run #7
Run #8
Run #9
Run #10
Run #11

## Slide 16: Conclusions
The MFIX simulation of the TRIGTM gasifier showed very good agreement with PSDF operating data over a broad range of operating conditions for Mississippi lignite fuel
  Syngas composition and temperature profiles are in good agreement with PSDF data
  Predicted pressure drops for all conditions match data well for most locations - except for the Lower Mixing Zone
    Model underpredicts the solids loading in the LMZ
Use of PC Coal Lab database and C3M software provides accurate devolatilization and gasification kinetics
  Kinetic parameters were accurate for all operating conditions
Improvement in prediction of LMZ solids loading is needed
  May be potential for size segregation - lower mixing zone could accumulate larger size particles from recycle flow
  Model may need to consider a distribution of sizes to allow for size segregation at the J-leg return
Notes: Carbon content in each size range is key as well.

## Slide 17: Thank you - Questions?
NETL Multiphase Flow Research Team
Develop and maintain numerical and physical models to promote understanding of multiphase flow physics critical to advanced energy and environmental systems
MFIX Suite of Multiphase Codes
Open Source Code – available to the public
Supported and validated
Over 3800 registered users from 73 countries and 250+ institutions
  70% University; 20% Industry; 10% NLs and misc.
Ongoing Code Development for increased:
  Accuracy
  Speed
  Multiphase physics capability
  Ease of use
2 updates per year on average
Industry Suggestions for Code Capability and Collaboration are Welcome!