## Slide 1: U.S. Department of Energy, National Energy Technology Laboratory’s (NETL) 2016 Workshop on Multiphase Flow Science Conversion of Petroleum Coke in a High-Pressure Entrained-Flow Gasifier: Comparison of CFD Model and Experiment
August 9, 2016
Allan Runstedtler, Robert Yandon, Marc Duchesne, Robin Hughes, Patrick Boisvert

## Slide 2: Entrained Flow Gasification

## Slide 3: CFD Model Validation
Experimental measurements of high-pressure gasifiers usually consist only of wall temperatures and outlet gas temperature and composition.
How should a CFD model be validated with this data?
The approach taken here is to compare the model predictions with measurements over a range of operating conditions comprising both favorable and unfavorable performance.
The CFD model should able to track the performance of the gasifier over the range of operating conditions, i.e., to predict higher and lower solid fuel conversion levels.

## Slide 4: Geometry
ACTIVELY COOLED TOP HEAD
Probe
Petroleum Coke & Carrier Gas (N2)
ACTIVELY COOLED TOP HEAD
Probe
WALL
THERMO-COUPLES
Modeled half-section with symmetry plane
Mesh consists of 1.5 million nodes, primarily hexahedral elements, refined near burner

## Slide 5: Petroleum Coke Analysis
Proximate Analysis (mass percent) | 
Volatiles | 12.7
Fixed Carbon | 82.2
Ash | 4.6
Moisture | 0.5
Ultimate Analysis (mass percent) | 
Carbon | 86.4
Hydrogen | 4.2
Sulphur | 6.1
Nitrogen | 1.8
Oxygen | 1.5

## Slide 6: Particle Size Distribution
A total of 30,000 particles were injected in 66 particle groups

## Slide 7: Model: Devolatilization
Devolatilization rate is modeled using a first-order Arrhenius rate equation, with the rate constants estimated from the PC Coal Lab® software
Volatile yield (weight loss on as-received basis) is 16.5%, implying a volatile yield factor of 1.3
Petroleum coke char composition after devolatilization (dry ash-free weight percent) predicted by PC Coal Lab® is C: 92.7%, H: 0.4%, O: 0.1%, N: 1.9%, S: 4.9%

## Slide 8: Model: Char Reactions
Char reaction stoichiometry:
  Char + 0.485 O2 → 0.918 CO + 0.0236 H2
  Char + 0.969 CO2 → 1.89 CO + 0.0236 H2
  Char + 0.969 H2O → 0.918 CO + 0.993 H2
Char reaction rates given by:

## Slide 9: Model: Char Reactions (continued)
Char reactivity calibration points were obtained using thermogravimetric analysis performed at CanmetENERGY
Reaction rates were estimated from PC Coal Lab® simulations of a drop tube furnace with the gasifier environment

## Slide 10: Model: Gaseous Reactions
Generally, the slower of eddy dissipation model (EDM) and finite rate chemistry (FRC)
Stoichiometry of the volatile oxidation reaction was obtained from PC Coal Lab® software, but no reaction rate was available. It was assumed that the volatile reaction was limited by turbulent mixing, using the eddy dissipation model.
The other gas phase reactions were
(EDM and FRC)
(FRC only)
Including the reaction, , produced little change in the results

## Slide 11: Model: Particle-Wall Interaction
For particles above 99% conversion, the approach used to account for particle-wall interactions is similar to the work by Richter et al.,
is the critical viscosity of 100 Pa·s and is the ash viscosity predicted using the approach from Kalmanovitch and Frank

## Slide 12: Model: Heat Transfer
Discrete transfer radiation model with 8 rays and composition-dependent gas radiative properties
Blackbody temperature of 135°C was applied to the outlet to represent the effect of the water quench zone below

## Slide 13: Model: Heat Transfer (continued)
Coupled 1-D conduction heat transfer calculation
Part of CFD calculation
Heat loss through wall

## Slide 14: Operating Conditions
Case | 1 (base case) | 2 (higher fuel rate) | 3 (lower pressure)
Duration (minutes) | 300 | 25 | 25
Fuel flow rate (kg/h) Standard deviation (kg/h) | 41.2 7.7 | 59.7 5.5 | 43.1 3.4
Steam flow rate (kg/h) Standard deviation (kg/h) | 10.7 0.9 | 10.2 0.8 | 10.9 0.3
Oxygen flow rate (kg/h) Standard deviation (kg/h) | 37.2 2.1 | 43.6 0.3 | 36.8 0.7
Gasifier pressure (kPa gauge) | 1500 | 1500 | 700
Steam supply temperature (°C) | 226.6 | 230.6 | 206.3
N2 flow (kg/h) for conveying fuel and for instrumentation ports | 12.1 | 11.1 | 7.2

## Slide 15: Results: Solid Conversion
Case 1 (base case) |  | Case 2 (higher fuel rate) |  | Case 3 (lower pressure) | 
CFD | Experiment | CFD | Experiment | CFD | Experiment
92.3 | 89.7 | 74.1 | 77.2 | 82.0 | 77.3
% Conversion of Solid to Gas
Iteration-to-iteration variability of 3% in the conversion rate was observed during the numerical solution for Case 3, suggesting some flow instability for this case.

## Slide 16: Results: Outlet Gas Composition
Case 1 (base case)
60
50
40
30
20
10
0

## Slide 17: Results: Outlet Gas Composition
Case 2 (higher fuel rate)
70
60
50
40
30
20
10
0

## Slide 18: Results: Outlet Gas Composition
Case 3 (lower pressure)
70
60
50
40
30
20
10
0

## Slide 19: Results: Wall Temperature
Case 1

## Slide 20: Note: Reactor Temperature Sensitivity
Adiabatic reactor temperature versus variation in fuel flow rate for Case 1

## Slide 21: Results: Temperature
Solid
Gas
2125
1705
1285
865
445
25
Temperature (°C)
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 22: Results: Velocity
15.0
11.25
7.5
3.75
0.0
Velocity (m/s)
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 23: Results: CO2 Molar Fraction
0.064
0.048
0.032
0.016
0.0
0.080
CO2 Molar Fraction
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 24: Results: Particle Concentration
0.005
0.004
0.003
0.002
0.001
0.0
Particle Average Volume Fraction
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 25: Results: CO Source
100
10
1
0.1
0.01
0.001
CO Source (kg/(m3·s))
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 26: Results: Particle Deposition on Wall
2.0
1.6
1.2
0.8
0.4
0.0
Particle Deposition Rate (g/(m2·s))
Case 1
(base case)
Case 2
(higher fuel rate)
Case 3
(lower pressure)

## Slide 27: Conclusions
The model predicted variation in solid fuel conversion over the range of conditions in agreement with the experimental findings, showing that it tracks a key gasifier performance indicator—conversion of solid fuel to gas and its dependence on burner and gasifier design and operating conditions.
The model provided further insight into the gasifier performance, showing that at the lower pressure operation, poor flow dynamics led to reduced solid fuel conversion.